## Slide 1
Nanomaterials and photonic solutions. Novel ‘at source’ approaches
to stop hospital-derived pharmaceuticals reaching the sewer network
Manuel-Thomas Valdivia
Where learning means more

## Slide 2
Sustainable
drug
elimination
Fenton H2O2
Ozone
UV disinfection
Photocatalysis vs conventional treatment
ROS

## Slide 3
1 Hospital-relevant drug selection
Antibiotic
Analgesic
Cytostatic
Statin
2 Drug detection method (ng/L)
Raman and mass spectroscopy
3 Photocatalytic bench-scale treatment
Amoxicillin
Paracetamol
Tamoxifen
Methotrexate
Simvastatin
4 Photocatalytic flow-through treatment
Carbon-based
support materials
H2O
H2O

## Slide 4
Chart: PARACETAMOL
| 0 | 5 | 10 | 20 | 30 | 40 | 50 | 75 | 100 | 200 | 300 | 400 | 500 | 600 | 800
 | 9129 | 9804 | 18580 | 20420 | 21250 | 21950 | 27910 | 45080 | 67030 | 77880 | 104300 | 110000 | 143100
Chart: AMOXICILLIN
| 0 | 5 | 10 | 20 | 30 | 40 | 50 | 75 | 100 | 200 | 300 | 400 | 500 | 800 | 1000
 | 5802 | 9151 | 10520 | 15050 | 18090 | 24570 | 46880 | 62230 | 80610 | 122100 | 147300
Chart: SIMVASTATIN
| 0 | 5 | 10 | 20 | 30 | 40 | 50 | 75 | 100 | 200 | 300 | 400 | 500 | 600 | 800 | 1000
 | 8089 | 9880 | 14630 | 17800 | 22810 | 29650 | 35990 | 46420 | 96770 | 135900 | 170700 | 225200 | 236400 | 345600 | 412400
Chart: TAMOXIFEN
| 0 | 5 | 10 | 20 | 30 | 40 | 50 | 75 | 100 | 200 | 300 | 400 | 500 | 600 | 800 | 1000
 | 7554 | 8492 | 10350 | 13320 | 15850 | 19160 | 24270 | 33520 | 61540 | 94880 | 123800 | 146900 | 170800 | 235500 | 284700
Chart: METHOTREXATE
| 0 | 5 | 10 | 20 | 30 | 40 | 50 | 75 | 100 | 200 | 300 | 400 | 500 | 600 | 800 | 1000
 | 15190 | 15260 | 19020 | 24820 | 31130 | 36170 | 46790 | 65820 | 116000 | 194900 | 255200 | 307500 | 351700 | 488500 | 569100
LOQ 90 ng/L
LOD 30 ng/L
Mass spectrometric detection of drugs at environmental concentrations (ng/L)

## Slide 5
Paracetamol <2 – 1369 198 6920
M.-T. Valdivia et al. Journal of Water Process Engineering 52 (2023)

## Slide 6
Photocatalytic bench-scale treatment
Chart: Paracetamol
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300
UV-light | 23.3586 | 16.7051 | 14.0465 | 10.5505 | 8.3567 | 3.8787 | 1.6379 | 0 | 0 | 0 | 0 | 0
UV-photolysis | 25.1958 | 26.0441 | 26.4682 | 26.4524 | 25.5371 | 26.7295 | 28.1995 | 26.1805 | 27.7622 | 26.0183 | 26.617 | 25.7029
Daylight photolysis | 26.1015 | 26.0484 | 25.9244 | 27.1726 | 27.1202 | 26.5782 | 26.5156 | 26.4063 | 26.7047 | 27.2439 | 26.7412 | 28.0622
100% drug elimination
after 2.5 h
100% drug elimination
after 2 h
Photocatalyst: Zinc Oxide
Chart: Amoxicillin
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270
 | 17.1769 | 11.653 | 7.5494 | 5.7064 | 3.437 | 1.9924 | 0 | 0 | 0 | 0 | 0 | 0
 | 20.3794 | 17.0701 | 16.9902 | 16.951 | 17.0295 | 18.9666 | 17.8357 | 19.676 | 17.5352 | 17.0568 | 16.6584 | 17.6594
 | 22.1348 | 18.1756 | 17.7516 | 17.1861 | 18.1727 | 16.6614 | 17.4278 | 17.6285 | 17.7131 | 18.7895 | 17.4855 | 17.4298
PHOTOCATALYTIC TREATMENT TIME (MIN)
Photolysis Control (UV-light - No Zinc Oxide)
Dark Control

## Slide 7
Chart: First order reaction rate
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300
UV-light | 0 | 0.33525 | 0.50859 | 0.7948 | 1.0279 | 1.7955 | 2.6576
Chart: photocatalytic treatment time (min)
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300
UV-light | 23.3586 | 16.7051 | 14.0465 | 10.5505 | 8.3567 | 3.8787 | 1.6379 | 0 | 0 | 0 | 0 | 0
Chart: photocatalytic treatment time (min)
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300
UV-light | 17.1769 | 11.653 | 7.5494 | 5.7064 | 3.437 | 1.9924 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: log10 (c0/ct)
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300
 | 0 | 0.388 | 0.8221 | 1.102 | 1.609 | 2.1542
Paracetamol
Amoxicillin
Test for 1st order reaction for photocatalytic drug elimination

## Slide 8
3.37 eV
1.24 eV
band gap
Zinc Oxide
Narrow band gap
UV-light effective
UV-light ineffective
How effective can metal oxide photocatalysts generate ROS ?
M.-T. Valdivia et al. Journal of Water Process Engineering 52 (2023)
Primary redox reactions in metal oxide – water interface:
O2 + e- = .O2-
(Reduction of oxygen to superoxide)
H2O + h+ = .OH
(Oxidation of water to hydroxyl radicals)
Wide band gap
Copper(II) oxide

## Slide 9
PHOTOCATALYTIC TREATMENT TIME (MIN)
ZnO
Photolysis Control
Dark Control
Paracetamol
Amoxicillin
Chart: CuO
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270
 | 25.0351 | 25.9263 | 26.6889 | 26.9452 | 27.1476 | 26.1298 | 26.2676 | 26.8835 | 25.6032 | 27.4457 | 26.3999 | 26.2682
 | 25.895 | 24.9119 | 25.6208 | 24.9999 | 26.111 | 25.911 | 26.1903 | 26.3299 | 25.7047 | 27.0284 | 28.3865 | 26.6781
 | 25.2119 | 25.9923 | 25.1331 | 25.8921 | 26.3476 | 26.3549 | 26.5756 | 25.9149 | 27.4496 | 27.4433 | 27.1645 | 27.3497
 | 22.716 | 25.6032 | 26.1828 | 26.4591 | 26.5159 | 26.3589 | 25.8164 | 26.5546 | 25.6247 | 27.249 | 27.3823 | 25.9105
Chart: drug concentration (mg/L)
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300
UV-light | 23.3586 | 16.7051 | 14.0465 | 10.5505 | 8.3567 | 3.8787 | 1.6379 | 0 | 0 | 0 | 0 | 0
UV-photolysis | 25.1958 | 26.0441 | 26.4682 | 26.4524 | 25.5371 | 26.7295 | 28.1995 | 26.1805 | 27.7622 | 26.0183 | 26.617 | 25.7029
Daylight photolysis | 26.1015 | 26.0484 | 25.9244 | 27.1726 | 27.1202 | 26.5782 | 26.5156 | 26.4063 | 26.7047 | 27.2439 | 26.7412 | 28.0622
Chart: 
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270
 | 17.1769 | 11.653 | 7.5494 | 5.7064 | 3.437 | 1.9924 | 0 | 0 | 0 | 0 | 0 | 0
 | 20.3794 | 17.0701 | 16.9902 | 16.951 | 17.0295 | 18.9666 | 17.8357 | 19.676 | 17.5352 | 17.0568 | 16.6584 | 17.6594
 | 22.1348 | 18.1756 | 17.7516 | 17.1861 | 18.1727 | 16.6614 | 17.4278 | 17.6285 | 17.7131 | 18.7895 | 17.4855 | 17.4298
No drug elimination
100% drug elimination
after 2 – 2.5 h

## Slide 10
.O2- forms a stable Tempone radical
with the spin-trap Tempone-H
1:1:1 hyperfine peak splitting
Pyrogallol:
ROS determination via Electron Paramagnetic Resonance spectroscopy (EPR)
Chart: time (min)
| 0 | 1 | 2 | 3 | 4 | 5
 | 8073 | 14249 | 20320 | 25443 | 29932
 | 11995 | 18559 | 29861 | 26092 | 29742
Pyrogallol Control
Tempone-H autooxidation

## Slide 11
Chart: time (min)
| 0 | 0.33333333333333331 | 0.66666666666666663 | 1 | 1.5 | 2 | 3 | 4 | 5
 | 402 | 282 | 320 | 376 | 468 | 480 | 457 | 504 | 522
 | 2081 | 5000 | 7200 | 10185 | 11599 | 11560
 | 2037 | 5240 | 10999 | 12247 | 14840 | 17228 | 19900 | 22040 | 23708
Chart: time (min)
| 0 | 0.33333333333333331 | 0.66666666666666663 | 1 | 1.5 | 2 | 3 | 4 | 5
 | 402 | 282 | 320 | 376 | 468 | 480 | 457 | 504 | 522
 | 2319 | 3364 | 4281 | 5546 | 6364 | 7239
 | 1205 | 2799 | 4120 | 5640 | 6887 | 7735 | 8600 | 11869 | 12323
ZnO
CuO
Photocatalytic .O2- generation
Tempone-H autooxidation
Dark
UV-light

## Slide 12
PHOTOCATALYTIC TREATMENT TIME (MIN)
ZnO
Photolysis Control
Dark Control
Paracetamol
Amoxicillin
Chart: CuO
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270
 | 25.0351 | 25.9263 | 26.6889 | 26.9452 | 27.1476 | 26.1298 | 26.2676 | 26.8835 | 25.6032 | 27.4457 | 26.3999 | 26.2682
 | 25.895 | 24.9119 | 25.6208 | 24.9999 | 26.111 | 25.911 | 26.1903 | 26.3299 | 25.7047 | 27.0284 | 28.3865 | 26.6781
 | 25.2119 | 25.9923 | 25.1331 | 25.8921 | 26.3476 | 26.3549 | 26.5756 | 25.9149 | 27.4496 | 27.4433 | 27.1645 | 27.3497
 | 22.716 | 25.6032 | 26.1828 | 26.4591 | 26.5159 | 26.3589 | 25.8164 | 26.5546 | 25.6247 | 27.249 | 27.3823 | 25.9105
Chart: drug concentration (mg/L)
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300
UV-light | 23.3586 | 16.7051 | 14.0465 | 10.5505 | 8.3567 | 3.8787 | 1.6379 | 0 | 0 | 0 | 0 | 0
UV-photolysis | 25.1958 | 26.0441 | 26.4682 | 26.4524 | 25.5371 | 26.7295 | 28.1995 | 26.1805 | 27.7622 | 26.0183 | 26.617 | 25.7029
Daylight photolysis | 26.1015 | 26.0484 | 25.9244 | 27.1726 | 27.1202 | 26.5782 | 26.5156 | 26.4063 | 26.7047 | 27.2439 | 26.7412 | 28.0622
Chart: 
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270
 | 17.1769 | 11.653 | 7.5494 | 5.7064 | 3.437 | 1.9924 | 0 | 0 | 0 | 0 | 0 | 0
 | 20.3794 | 17.0701 | 16.9902 | 16.951 | 17.0295 | 18.9666 | 17.8357 | 19.676 | 17.5352 | 17.0568 | 16.6584 | 17.6594
 | 22.1348 | 18.1756 | 17.7516 | 17.1861 | 18.1727 | 16.6614 | 17.4278 | 17.6285 | 17.7131 | 18.7895 | 17.4855 | 17.4298
No drug elimination
100% drug elimination
after 2 – 2.5 h

## Slide 13
.OH forms a stable DMPO-OH adduct
with the spin-trap: 5,5-dimethyl-1-pyrroline-N-oxide (DMPO)
1:2:2:1 hyperfine peak splitting
Fenton Reaction:
Fe2+ + H2O2 -> Fe3+ + .OH
ROS determination via Electron Paramagnetic Resonance spectroscopy (EPR)
Chart: time (min)
| 0 | 1 | 2 | 3 | 4 | 5 | 6
 | 3000 | 7597 | 14403 | 19642 | 22706 | 24629 | 26784
 | 1853 | 1564 | 1719 | 3247 | 2462 | 1518 | 1579 | 1967 | 1390 | 1622
Fenton Control
DMPO autooxidation
(pH 3)

## Slide 14
ZnO
CuO
Photocatalytic .OH generation

## Slide 15
PHOTOCATALYTIC TREATMENT TIME (MIN)
ZnO
Photolysis Control
Dark Control
Paracetamol
Amoxicillin
Chart: CuO
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270
 | 25.0351 | 25.9263 | 26.6889 | 26.9452 | 27.1476 | 26.1298 | 26.2676 | 26.8835 | 25.6032 | 27.4457 | 26.3999 | 26.2682
 | 25.895 | 24.9119 | 25.6208 | 24.9999 | 26.111 | 25.911 | 26.1903 | 26.3299 | 25.7047 | 27.0284 | 28.3865 | 26.6781
 | 25.2119 | 25.9923 | 25.1331 | 25.8921 | 26.3476 | 26.3549 | 26.5756 | 25.9149 | 27.4496 | 27.4433 | 27.1645 | 27.3497
 | 22.716 | 25.6032 | 26.1828 | 26.4591 | 26.5159 | 26.3589 | 25.8164 | 26.5546 | 25.6247 | 27.249 | 27.3823 | 25.9105
Chart: drug concentration (mg/L)
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300
UV-light | 23.3586 | 16.7051 | 14.0465 | 10.5505 | 8.3567 | 3.8787 | 1.6379 | 0 | 0 | 0 | 0 | 0
UV-photolysis | 25.1958 | 26.0441 | 26.4682 | 26.4524 | 25.5371 | 26.7295 | 28.1995 | 26.1805 | 27.7622 | 26.0183 | 26.617 | 25.7029
Daylight photolysis | 26.1015 | 26.0484 | 25.9244 | 27.1726 | 27.1202 | 26.5782 | 26.5156 | 26.4063 | 26.7047 | 27.2439 | 26.7412 | 28.0622
Chart: 
| 0 | 15 | 30 | 45 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270
 | 17.1769 | 11.653 | 7.5494 | 5.7064 | 3.437 | 1.9924 | 0 | 0 | 0 | 0 | 0 | 0
 | 20.3794 | 17.0701 | 16.9902 | 16.951 | 17.0295 | 18.9666 | 17.8357 | 19.676 | 17.5352 | 17.0568 | 16.6584 | 17.6594
 | 22.1348 | 18.1756 | 17.7516 | 17.1861 | 18.1727 | 16.6614 | 17.4278 | 17.6285 | 17.7131 | 18.7895 | 17.4855 | 17.4298
No drug elimination
100% drug elimination
after 2 – 2.5 h

## Slide 16
Summary
CuO shows no photocatalytic effect on 2 test drugs
CuO does not generate .OH during photocatalysis
ZnO eliminates 2 test drugs after 2 - 2.5 h
ZnO generates both .O2- and .OH during photocatalysis
Conclusion
.OH may be the principal radical species responsible
for photocatalytic drug elimination

## Slide 17
Thank you
Supervisory Team: Prof Ian Megson, Prof Alistair Kean, Dr Mark Taggart, Dr Szabolcs Pap