## Slide 1
Water Purification in Rural India Using Sunlight and Low-Cost Materials
Victoria Porley
Supervisors:
Prof. Neil Robertson & Dr Efthalia Chatzisymeon

## Slide 2: Water as a Critical Resource
“By 2050, at least one in four people is likely to live in a country affected by chronic or recurring shortages of fresh water” – United Nations
United Nations, http://www.un.org/sustainabledevelopment/sustainable-development-goals/
WHO - approximately 30% of the global population are currently without a safe source of drinking water, which in turn leads to around half a million entirely preventable deaths a year
Motivates Sustainable Development Goal 6 – To ensure availability and sustainable management of water and sanitation for all by 2030

## Slide 3: Addressing the Problem
United Nations, http://www.un.org/sustainabledevelopment/sustainable-development-goals/
There is a clear necessity to develop a method of water purification for those living in areas most at risk of depending on poor quality water sources. This must be:
  Safe
  Cheap
  Simple
  Reliable
  Robust
  Point-of-source
Solar-powered water purification?

## Slide 4: Solar Disinfection (SODIS)
The Sun’s natural disinfecting ability is utilised globally in areas where water resources are unsafe and resources are limited.
Photocatalysis – using light to initiate chemical reactions
Reduces bacterial content, but rates slow and doesn’t remove any chemical pollutants
R. Meierhofer and G. Landolt, Desalination, 2009, 248, 144–151

## Slide 5: The Photocatalysis Process
Encyclopedia of Nanoscience and Nanotechnology, Yamashita and Takeuchi, American Scientific Publishers, 9, 2004
TiO2
Hazardous Materials
Dyes
Bacteria
Pharmaceuticals
Detergents
Endocrine disruptors
CO2
H2O
UV

## Slide 6: Photocatalysis for Water Purification
Advantage | Disadvantage
Low operational and installation cost | High energy lamps needed
Non-professional and unmanned operation is possible | Catalyst recovery from water
Can avoid use of dangerous chemicals | 
Can work on small and large scale | 
Tackle with:
Solar photocatalysis
Immobilising the catalyst on a support

## Slide 7: Previous Work in The Robertson Group
G. Odling and N. Robertson, ChemPhysChem, 2016, 17, 2872-2880
G. Odling and N. Roberston, ChemPhysChem, 2017, 18, 728-735
G. Odling, E. Chatzisymeon and N. Robertson, Cat. Sci. Technol., 2018, 8, 829–839.
G. Odling, A. Ivaturi, E. Chatzisymeon and N. Robertson, ChemCatChem, 2017, 9, 1–11
G. Odling, Z. Y. Pong, G. Gilfillan, C. R. Pulham and N. Robertson, Environ. Sci.: Water Res. Technol., 2018, 4, 2170–2178

## Slide 8: Immobilising the Photocatalysts
This requires considering:
The material itself
The structure
The processing method and conditions
One of the most popular materials to use is glass. Successful laboratory tests have been conducted on etched glass beads.

## Slide 9: Solar Photocatalysis
Chemical modifications have been performed to alter the band gap of the titania-based photocatalyst materials, improving the visible light absorption
Bi4Ti3O12 (BTO)
Has a narrower bandgap than titania (~410 nm)  Improved visible light absorption
Presence of a heterojunction between the two materials  reduces charge recombination
Cai, Y et al, Environ. Sci.: Nano,5, 2631-2640, 2018
G. Odling, Z. Y. Pong, G. Gilfillan, C. R. Pulham and N. Robertson, Environ. Sci.: Water Res. Technol., 2018, 4, 2170–2178

## Slide 10: Real-world Testing in India
Over March and April, 2019, field tests were conducted at the Indian Institute of Technology Kharagpur in West Bengal
Aim: to investigate the efficacy of TiO2 and BTO coated on glass beads for water purification in a real-world context

## Slide 11: Methodology
  Collect 5 different water sources
  Expose to light for 3 hours in 500 mL plastic bottles filled with 45g of beads (monolayer)
  Analyse – bacterial content, total dissolved solids (TDS), salt and conductivity
  Investigate the effect of exposure time by irradiating for 1, 3 and 5 hours
  Repeat each run 3 times
1 Hour
3 Hours
5 Hours
BTO
No Catalyst
TiO2

## Slide 12: Water Sources
Village well 1 –Porapara (W1P)
Village well 2 – IIT KGP Boundary Wall (W2B)
This source was used for the time interval tests.
Campus Tap Water (CW)
Tube Well Water (TW)
Social/Time Water (STW)

## Slide 13: Results – General Observations
No change to TDS, salt or conductivity
Fluctuations in results were clear with changes in the weather
Irreversible damage to beads – became visibly darker
  Would need to be replaced more frequently
  Usual cleaning method insufficient

## Slide 14: Results – TDS, Salt and Conductivity Levels
WHO - TDS should be below 1000 ppm to be potable. Optimum between 300 and 600 ppm. All samples fell below the upper limit

## Slide 15: Results – Bacterial Colony Counts
Raw
BTO
TiO2
No Catalyst
TiO2 Glass Tube
W2B had highest raw bacterial count
Consistently fluctuating results seen from glass tube reactor – difficult to keep clean and controlled
BTO showed dip in counts – most effective treatment method
No catalyst and TiO2 results often comparable
 | Colony Forming Units per mL (CFU/mL) |  |  |  | 
 | W1P | W2B | CW | TW | STW
Raw | 1658 | 2438 | 1310 | 2375 | 342
No Catalyst | 400 | 283 | 225 | 1358 | 513
BTO | 388 | 125 | 563 | 475 | 63
TiO2 | 994 | 342 | 63 | 1725 | 438
TiO2 glass 300mL | 2400 | 125 | 500 | 50 | 2775

## Slide 16: Results – Bacterial Colony Counts
Chart: Change in Bacterial Cultures with Time
| 0 | 1 | 3 | 5
No Cat | 1 | 0.26222 | 0.14222 | 0.031111
BTO | 1 | 0.093333 | 0.044444 | 0.017778
TiO2 | 1 | 0.16667 | 0.06 | 0.026667
Chart: Log of Change in Bacterial Cultures with Time
| 0 | 1 | 3 | 5
No Cat | 0 | 1.3386 | 1.9504 | 3.4702
BTO | 0 | 2.3716 | 3.1135 | 4.0298
TiO2 | 0 | 1.7918 | 2.8134 | 3.6243
WHO - E.Coli levels should be at 0 CFU/mL for potable water. This was achieved for some samples after 5 hours irradiation, but not consistently. BTO showed the fastest rate and lowest final CFU counts

## Slide 17: Results – Bacterial Colony Counts
The Degradation Efficiency (DE) was calculated for each treatment type:
The following results were obtained:
  No catalyst (SODIS alone) = 68%
  BTO = 81%
  TiO2 = 60%
  TiO2 glass tube = 33%
These values demonstrate the superior function of the BTO catalyst, as well as the risk of using an insufficient catalyst and system contamination

## Slide 18: Further Interesting Findings
Though the treatments show promise, there may be more economic and social blocks to its implementation
  UV Filtration site used in Porapara, but with resistance despite the low cost of water.
Bisleri bottles were used for the experiment – one of the largest brands for bottled water in India, and also one of the worst for microplastic leaching (https://orbmedia.org/sites/default/files/FinalBottledWaterReport.pdf

## Slide 19: Conclusions
For the water sources around the campus, the main issues seem to be bacterial content and hardness
Treatment shows good potential for removing bacteria, but not for altering hardness (as expected)
BTO provided the best rates of purification and to the largest extent, but is not yet quick enough yet
Further optimisation is required to improve the efficiency of the catalysts so the effects of poor weather and contamination to the system are not so significant

## Slide 20: Acknowledgements
Supervisors:
Edinburgh – Prof. Neil Robertson and Efthalia Chatzisymeon (as well as the whole Robertson group)
India – Prof. B.C. Meikap, Dr Somnath Goshal, Prof. Pulak Mishra